## Slide 1: Towards Image Based Modelling of Composite Li-ion Electrodes
James Le Houx, Denis Kramer, Richard Wills

## Slide 2: Contents
Research challenge
Why use an image-based model?
Imaging methods (μVis Laboratory)
Modelling Technique
Initial scaling results
Conclusion

## Slide 3: Research Challenge
To develop an image based, multi-physics computational framework capable of modelling lithium ion batteries
Understand how thermal fields propagate through microstructure
Imaging of Li-ion electrode microstructure
Solution of multi-physics partial differential equations
Generate report to characterise battery performance

## Slide 4: Bruggeman Correlation

## Slide 5: Bruggeman Correlation
Current Li-ion modelling assumes electrodes are homogenous structures through the use of the Bruggeman correlation
This correlation has been shown to be invalid for heterogeneous structures [2]
Figure 1: SEM image of a commercial lithium iron phosphate electrode [1]
[1]: Kashkooli, A. (2016) Multiscale Modeling of lithium-ion battery electrodes based on nano-scale X-ray computed tomography, Journal of Power Sources 307 496-509
[2]: Tjaden, B., Cooper, S. J., Brett, D. J., Kramer, D., & Shearing, P. R. (2016). On the origin and application of the Bruggeman correlation for analysing transport phenomena in electrochemical systems. Current opinion in chemical engineering, 12, 44-51.

## Slide 6: Structured Electrodes
[1]: Nishihara, H., & Kyotani, T. (2012). Templated nanocarbons for energy storage. Advanced Materials, 24(33), 4473-4498.
[2]: Lee, S. W., Yabuuchi, N., Gallant, B. M., Chen, S., Kim, B. S., Hammond, P. T., & Shao-Horn, Y. (2010). High-power lithium batteries from functionalized carbon-nanotube electrodes. Nature nanotechnology, 5(7), 531.
Figure 1: Scheme of the ice-templating method [1]

## Slide 7: Imaging Methods
SEM has all been used in electrode analysis however they all miss 3D volumetric properties that are of interest to us. ~10nm
Focused Ion Beam (FIB) allows 3d volumetric properties in the nano-scale, but is a destructive method. ~5nm
X-ray tomography allows for the multiple length scales required whilst being a non-destructive imaging method. ~50nm

## Slide 8: μVis Laboratory
Figure 1: Photograph of the University of Southampton’s Zeiss 160 kVp Versa 510 [1]
[1] Zeiss 160 kVp Versa 510, μVis, https://www.southampton.ac.uk/muvis/about/equipment/versa.page Date Accessed: 10/06/18
Voxel Size: 70nm
Pixel Detector : 2048 x 2048

## Slide 9: CT Imaging of Electrodes
Figure 1: Individual tomographic slice of a TiO2 layer on a carbon polymer substrate, voxel size of 481nm
50μm
Obtain tomography of electrode structure
Air
TiO2
Carbon Polymer

## Slide 10: CT Imaging of Electrodes
Figure 1: Volumetric rendering of a thresholded TiO2 layer on a carbon polymer substrate, ~108 voxels, size of 481nm
50μm
Obtain tomography of electrode structure
Threshold the data into regions of interest through post-processing

## Slide 11: Similar Research
[1]: Kashkooli, A. (2016) Multiscale Modeling of lithium-ion battery electrodes based on nano-scale X-ray computed tomography, Journal of Power Sources 307 496-509
[2]: Cooper, S. J., Bertei, A., Shearing, P. R., Kilner, J. A., & Brandon, N. P. (2016). TauFactor: An open-source application for calculating tortuosity factors from tomographic data. SoftwareX, 5, 203-210.
Figure 1: Finite element mesh from Kashkooli’s simulation [1]
Sample Size: 750nm x 750nm x 750nm

## Slide 12: Similar Research
[1]: Kashkooli, A. (2016) Multiscale Modeling of lithium-ion battery electrodes based on nano-scale X-ray computed tomography, Journal of Power Sources 307 496-509
[2]: Cooper, S. J., Bertei, A., Shearing, P. R., Kilner, J. A., & Brandon, N. P. (2016). TauFactor: An open-source application for calculating tortuosity factors from tomographic data. SoftwareX, 5, 203-210.
Figure 1: Tortuosity calculation from Taufactor [2]

## Slide 13: Finite Differences vs Finite Element
[1] Lecture 24 – Introduction to Variational Methods, CEM, https://www.youtube.com/watch?v=BddajYoBHiI Date Accessed: 19/03/18

## Slide 14: Types of Structured Mesh
Mesh Distortion (Biasing)
[1]: Guarrasi, M. (2015) An introduction to Adaptive Mesh Refinement (AMR): Numerical Methods and Tools, Supercomputing Applications and Innovation

## Slide 15: Types of Structured Mesh
Mesh Distortion (biasing)
Point-wise (tree based)
[1]: Guarrasi, M. (2015) An introduction to Adaptive Mesh Refinement (AMR): Numerical Methods and Tools, Supercomputing Applications and Innovation

## Slide 16: Types of Structured Mesh
Mesh Distortion (biasing)
Point-wise (tree based)
Block-structured
In block-structured AMR the solution is defined on a hierarchy of levels of resolution – a union of rectangular grids which can change dynamically.
[1]: Guarrasi, M. (2015) An introduction to Adaptive Mesh Refinement (AMR): Numerical Methods and Tools, Supercomputing Applications and Innovation

## Slide 17: Block Structured Adaptive Mesh
Figure 1: A depiction of the Kelvin-Helmholtz instability using a 3 levelled adaptive mesh [1]
[1] Why Block Structured AMR?, AMReX, https://amrex-codes.github.io/overview.html Date Accessed: 19/03/18

## Slide 18: How does AMReX work?
Fortran PDE Thermal Kernel
Fortran PDE Electrochem Kernel
Fortran PDE Diffusion Kernel
Fortran PDE Electrical Kernel
C++ Wrapper used to call Fortran subroutines and AMReX library
MPI used to distribute to multinode HPC

## Slide 19: Partial Differential Equations
To model a li-ion electrode a number of physical fields need to be considered:
  Diffusion
  Thermal (Heat equation)
  Electrochemical (Butler-Volmer equation)
  Electrical (Ohm’s aw)
Our initial model solves for diffusion

## Slide 20: Programme Workflow
Obtain tomography of electrode structure
Threshold the data into regions of interest through post-processing
Calculation of tortuosity factor
(1)
[1] Grathwohl, P. (2012). Diffusion in natural porous media: contaminant transport, sorption/desorption and dissolution kinetics (Vol. 1). Springer Science & Business Media.
Eq 1 [1]: where is effective diffusivity, is intrinsic diffusivity and is the volume fraction of the conducting phase

## Slide 21: Programme Workflow
Obtain tomography of electrode structure
Threshold the data into regions of interest through post-processing
Calculation of tortuosity factor
(2)
[1]: Cooper, S. J., Bertei, A., Shearing, P. R., Kilner, J. A., & Brandon, N. P. (2016). TauFactor: An open-source application for calculating tortuosity factors from tomographic data. SoftwareX, 5, 203-210.
Eq 2,3 [1]: where is the flow through the pore network, is the flow a control volume, and are the area and length; and is the concentration of diffusing species
(3)

## Slide 22: Future Work
Scaling analysis comparison with Taufactor
Further CT imaging of electrode structure
Chart: Number of Threads
| 64 | 32 | 16 | 8 | 4 | 2 | 1
MPI Iridis | 16.7394 | 21.3847 | 31.995 | 41.8966 | 68.8045 | 129.7887 | 205.6138
OpenMP Iridis | 34.6627 | 51.0115 | 73.2336 | 112.1013 | 205.6138
Figure 1: Scaling analysis for solution to heat equation problem with embedded boundary

## Slide 23: Conclusions
An image based modelling framework for lithium-ion batteries has started development
Initial results show the code scales well with an increase in threads
50μm

## Slide 24: Any questions?